ABS AQ43 STEEL PLATE

Gangsteel is specialized in supplying ABS Extra high strength steel plate in ABS Grade AQ43. For more information of Grade AQ43 steel plate, please check them in following:

| ABS AQ43 Extra high Strength Chemical Composition in Tempering and Quenching |
| --- |
| Grade | The Element Max (%) |
|  | C | Si | Mn | P | S | N |
| ABS AQ43 | 0.21 | 0.55 | 1.7 | 0.035 | 0.035 | 0.02 |

Crack Sensitivity:  Pcm = (C+Si/30+Mn/20+Cu/20+Ni/60+Cr/20+Mo/15+V/10+5B)%
Carbon Equivalent:  Ceq = 【C+Mn/6+(Cr+Mo+V)/5+(Ni+Cu)/15】%

| ABS AQ43 Extra high strength property in tempering and quenching |
| --- |
| Grade | Mechanical Property | Charpy V Impact Test |
|  | Yield | Tensile | Elongation | Degree | Energy 1 | Energy 2 |
|  | Min Mpa | Mpa | Min % |  | J | J |
| ABS AQ43 | 420 | 530-680 | 18 | 0 | 41 | 27 |
| Note: Energy 1 is transverse impact test, Energy 2 is longitudinal |

Boiler steel plates | Alloy steel plates | High strength plate| Carbon steel plate

| Equivalent steel grade of ABS AQ43 |
| --- |
| DNV | GL | LR | BV | CCS | NK | KR | RINA |
| NV A420 | GL-A420 | LR/AH42 | BV/A420 | CCS/A420 | K A43 | R A43 | RI/A420 |

If you need more stock steel plates in shipbuilding steel plate, please click warehouse sizes.