ABS AQ47 STEEL PLATE

Gangsteel is specialized in supplying ABS Extra high strength steel plate in ABS Grade AQ47. For more information of Grade AQ47 steel plate, please check them in following:

| ABS AQ47 Extra high Strength Chemical Composition in Tempering and Quenching |
| --- |
| Grade | The Element Max (%) |
|  | C | Si | Mn | P | S | N |
| ABS AQ47 | 0.21 | 0.55 | 1.7 | 0.035 | 0.035 | 0.02 |

Crack Sensitivity:  Pcm = (C+Si/30+Mn/20+Cu/20+Ni/60+Cr/20+Mo/15+V/10+5B)%
Carbon Equivalent:  Ceq = 【C+Mn/6+(Cr+Mo+V)/5+(Ni+Cu)/15】%

| ABS AQ47 Extra high strength property in tempering and quenching |
| --- |
| Grade | Mechanical Property | Charpy V Impact Test |
|  | Yield | Tensile | Elongation | Degree | Energy 1 | Energy 2 |
|  | Min Mpa | Mpa | Min % | 0 | J | J |
| ABS AQ47 | 460 | 570-720 | 17 |  | 31 | 46 |
| Note: Energy 1 is transverse impact test, Energy 2 is longitudinal |

Boiler steel plates | Alloy steel plates | High strength plate| Carbon steel plate

| Equivalent steel grade of ABS AQ47 |
| --- |
| DNV | GL | LR | BV | CCS | NK | KR | RINA |
| NV A460 | GL-A460 | LR/AH46 | BV/A460 | CCS/A460 | K A47 | R A47 | RI/A460 |

If you need more stock steel plates in shipbuilding steel plate, please click warehouse sizes.