ABS FQ56 STEEL PLATE

Gangsteel is specialized in supplying ABS Extra high strength steel plate in ABS Grade FQ56. For more information of Grade FQ56 steel plate, please check them in following:

| ABS FQ56 Extra high Strength Chemical Composition in Tempering and Quenching |
| --- |
| Grade | The Element Max (%) |
|  | C | Si | Mn | P | S | N |
| ABS FQ56 | 0.18 | 0.55 | 1.6 | 0.025 | 0.025 | 0.02 |

Crack Sensitivity:  Pcm = (C+Si/30+Mn/20+Cu/20+Ni/60+Cr/20+Mo/15+V/10+5B)%
Carbon Equivalent:  Ceq = 【C+Mn/6+(Cr+Mo+V)/5+(Ni+Cu)/15】%

| ABS FQ56 Extra high strength property in tempering and quenching |
| --- |
| Grade | Mechanical Property | Charpy V Impact Test |
|  | Yield | Tensile | Elongation | Degree | Energy 1 | Energy 2 |
|  | Min Mpa | Mpa | Min % | -60 | J | J |
| ABS FQ56 | 550 | 670-835 | 16 |  | 37 | 55 |
| Note: Energy 1 is transverse impact test, Energy 2 is longitudinal |

Boiler steel plates | Alloy steel plates | High strength plate| Carbon steel plate

| Equivalent steel grade of ABS FQ56 |
| --- |
| DNV | GL | LR | BV | CCS | NK | KR | RINA |
| NV F550 | GL-F550 | LR/FH55 | BV/F550 | CCS/F550 | K F56 | R F56 | RI/F550 |

If you need more stock steel plates in shipbuilding steel plate, please click warehouse sizes.