WEL-TEN540 Weldable high tensile strength steel plate

Gangsteel supply WEL-TEN540 Steel plate from thickness 2mm to 300mm.Width from 1500*3900mm, WEL-TEN540 Series is high tensile and superior weldability steel featuring a rich variety of product categories. It has a wide range of applications, including pressure vessels, oil storage tanks, penstock, bridges, buildings, construction equipment and industrial equipment.

WEL-TEN540 Chemical requirement

| Grade | Chemical requirement or element Max % |
| --- | --- |
|  | C | Si | Mn | P | S | Cu | Ni | Cr | Mo | V | Nb | Ti | B |
| WEL-TEN540 | 0.2 | 0.55 | 1.7 | 0.035 | 0.035 | - | - | - | - | - | - | - | - |

WEL-TEN540 Property in tensile and yield strength, and impact test requirement

| Grade | Property | Impact test |
| --- | --- | --- |
| WEL-TEN540 | Yield Mpa Min | Tensile Mpa | Elongation | Min J |
|  | Thickness mm | Thickness mm |  | Degree |
|  | 50 | 50-100 | 100-150 | 50 | 50-100 | 10-150 | % | 0 | -20 | -40 | -60 |
|  | 355 |  |  | 540 |  | 23 | 47 |  |  |  |

HENAN GANG IRON AND STEEL CO.,LTD Supply WEL-TEN540 in about 3000tons stock for many thickness and sizes. If you have requirement for stock or new plate WEL-TEN540 requirement, please feel free to contact us or email to us by admin@gangsteel.com