A302GRB MR0175,A302GRB Steel,A302GRB HIC,A302GRB NACE

GANGSTEEL Bolier Plate Factory are specialized in producing and exporting ASTM A302/A302M A302GRB NACE MR0175, MR0103 Boiler steel plate, Low alloy and high strength steel plate,                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                  heavy plate and wide, heavy plate, Which is a large steel plate supplier mill at GANGSTEEL Group.

A302GRB,ASTM A302GRB,A302GRB Steel Plate,A302GRB HIC,A302GRB Nace

Tags: A302GRB,ASTM A302GRB,A302GRB Steel Plate,A302GRB steel factory, A302GRB adopt standard, A302GRB Heat treatment, A302GRB Technical delivery condition, A302GRB Chemical, A302GRB Mechanical property, A302GRB Price, A302GRB CEV, A302GRB Impact degree, A302GRB impact energy, A302GRB Supplier,A302GRB Specification, A302GRB properties, Material A302GRB N, A302GRB Material, ASTM A302GRB, A302GRB Steel, A302GRB Yield, A302GRB plate, A302GRB HIC, A302GRB NACE MR0175, A302GRB ISO 15156, A302GRB NACE MR0103, A302GRB SSC

Keyword: A302GRB,ASTM A302GRB,A302GRB Steel,A302GRB HIC,A302GRB NACE

- A302GRB Adopt standard: A302/A302M  Standard Specification for High-Strength Low-Alloy Columbium-Vanadium Structural Steel

- A302GRB Specification:  Thickness: 1mm to 100mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

- Third Party Inspection for A302GRB: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

- A302GRB Chemical composition % of the Product analysis of grade

| Grade | C % | Si % | Mn % | P % | S % | V % | AL % | Cr % |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| A302GrB | 0.20-0.25 | 0.13-0.45 | 1.07-1.62 | 0.035 | 0.035 |  |  |  |
|  | Cu % | Mo % | Nb % | Ni % | Ti % | Tungsten |  |  |
|  |  | 0.41-0.64 |  |  |  |  |  |  |

- A302GRB Mechanical Property

| Grade | Thickness(mm) | Min Yield | Tensile | Elongation | Min Impact Energy |
| --- | --- | --- | --- | --- | --- |
| A302GrB | 6-50 | 345 Mpa | 550-690 Mpa | 18% |  |  |
|  | 50-200 | 345 Mpa | 550-690 Mpa | 15% |  |  |

GANGSTEEL also could supply super thick steel plate from 100mm to 300mm, certified by TUV, SGS, CE and nine classification societies: ABS, DNV, LR, GL, BV, KR, RINA, CCS, NK.

At competitive price, better quality, faster delivery and better service in supply steel plate in China

GANGSTEEL has a strong relationship with our mill. We can supply ASTM A302GRB steel material directly at our mill ex-factory prices. Each plate has the Mill Certificate Test EN 10204 3.1/3.2 Version.

- A302GRB Delivery Time Or Lead Time: 15-30days

- A302GRB Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

- If you have any requirement in steel plate for A302GRB, whether the new plate or stock list of material, please feel free to contact us by email of calling.

- If you had any question at our plate or service. Please contact our after service department to get faster reply.

GANGSTEEL Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to GANGSTEEL Group and any requirement in steel material, please feel free to contact us.

GANGSTEEL Bolier Plate Factory are specialized in producing and exporting A302/A302M  A302GRB NACE MR0175, MR0103 Boiler steel plate, Low alloy and high strength steel plate,                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                  heavy plate and wide, heavy plate, Which is a large steel plate supplier mill at GANGSTEEL Group.

A302GRB,ASTM A302GRB,A302GRB Steel Plate,A302GRB HIC,A302GRB Nace

Tags: A302GRB,ASTM A302GRB,A302GRB Steel Plate,A302GRB steel factory, A302GRB adopt standard, A302GRB Heat treatment, A302GRB Technical delivery condition, A302GRB Chemical, A302GRB Mechanical property, A302GRB Price, A302GRB CEV, A302GRB Impact degree, A302GRB impact energy, A302GRB Supplier,A302GRB Specification, A302GRB properties, Material A302GRB N, A302GRB Material, ASTM A302GRB, A302GRB Steel, A302GRB Yield, A302GRB plate, A302GRB HIC, A302GRB NACE MR0175, A302GRB ISO 15156, A302GRB NACE MR0103, A302GRB SSC