A515 GR 60 MR0175,A515 GR 60 Steel,A515 GR 60 HIC,A515 GR 60 NACE

Gangsteel Bolier Plate Factory are specialized in producing and exporting ASTM A515 GR 60 A515 GR 60 NACE MR0175, MR0103 Boiler steel plate, Low alloy and high strength steel plate,                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                  heavy plate and wide, heavy plate, Which is a large steel plate supplier mill at Gangsteel Group.

A515 GR 60,ASTM A515 GR 60,A515 GR 60 Steel Plate,A515 GR 60 HIC,SA537GR70 Nace

Tags: A515 GR 60,ASTM A515 GR 60,A515 GR 60 Steel Plate,A515 GR 60 steel factory, A515 GR 60 adopt standard, A515 GR 60 Heat treatment, A515 GR 60 Technical delivery condition, A515 GR 60 Chemical, A515 GR 60 Mechanical property, A515 GR 60 Price, A515 GR 60 CEV, A515 GR 60 Impact degree, A515 GR 60 impact energy, A515 GR 60 Supplier,A515 GR 60 Specification, A515 GR 60 properties, Material A515 GR 60 N, A515 GR 60 Material, ASME A515 GR 60, A515 GR 60 Steel, A515 GR 60 Yield, A515 GR 60 plate, A515 GR 60 HIC, A515 GR 60 NACE MR0175, A515 GR 60 ISO 15156, A515 GR 60 NACE MR0103, A515 GR 60 SSC

Keyword: A515 GR 60,ASTM A515 GR 60,A515 GR 60 Steel,A515 GR 60 HIC,A515 GR 60 NACE

- A515 GR 60 Adopt standard: ASTM A515 GR 60 Standard Specification for High-Strength Low-Alloy Columbium-Vanadium Structural Steel

- A515 GR 60 Specification:  Thickness: 1mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

- Third Party Inspection for A515 GR 60: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

- A515 GR 60 Chemical composition % of the Product analysis of grade

| A515 grade 60 Chemical Composition |
| --- |
| Grade | The Element Max (%) |
|  | C | Mn | P | S | Si |
| A515 GR 60 | 0.24-0.31 | 0.98 | 0.035 | 0.035 | 0.13-0.45 |

- A515 GR 60 Mechanical Property

| Grade | A515 GR 60 Mechanical Property |
| --- | --- |
|  | Thickness | Yield | Tensile | Elongation |
| A515 GR 60 | mm | Min Mpa | Mpa | Min % |
|  | 200 | 220 | 415-550 | 21 |
|  | 50 |  |  | 25 |

ASTM A515 GR 60 plates 40mm and under in thickness is normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both. ASTM A515 GR 60 grade plates over 50mm in thickness shall be normalized.

- A515 GR 60 Delivery Time Or Lead Time: 15-30days

- A515 GR 60 Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

- If you have any requirement in steel plate for A515 GR 60, whether the new plate or stock list of material, please feel free to contact us by email of calling.

- If you had any question at our plate or service. Please contact our after service department to get faster reply.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting ASTM A515 GR 60 A515 GR 60 NACE MR0175, MR0103 Boiler steel plate, Low alloy and high strength steel plate,                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                  heavy plate and wide, heavy plate, Which is a large steel plate supplier mill at Gangsteel Group.

A515 GR 60,ASTM A515 GR 60,A515 GR 60 Steel Plate,A515 GR 60 HIC,A515 GR 60 Nace

Tags: A515 GR 60,ASTM A515 GR 60,A515 GR 60 Steel Plate,A515 GR 60 steel factory, A515 GR 60 adopt standard, A515 GR 60 Heat treatment, A515 GR 60 Technical delivery condition, A515 GR 60 Chemical, A515 GR 60 Mechanical property, A515 GR 60 Price, A515 GR 60 CEV, A515 GR 60 Impact degree, A515 GR 60 impact energy, A515 GR 60 Supplier,A515 GR 60 Specification, A515 GR 60 properties, Material A515 GR 60 N, A515 GR 60 Material, ASME A515 GR 60, A515 GR 60 Steel, A515 GR 60 Yield, A515 GR 60 plate, A515 GR 60 HIC, A515 GR 60 NACE MR0175, A515 GR 60 ISO 15156, A515 GR 60 NACE MR0103, A515 GR 60 SSC