SA516GR65 MR0175,SA516GR65 Steel,SA516GR65 HIC,SA516GR65 NACE

Gangsteel Bolier Plate Factory are specialized in producing and exporting ASME SA516 SA516GR65 NACE MR0175, MR0103 Boiler steel plate, Low alloy and high strength steel plate,                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                  heavy plate and wide, heavy plate, Which is a large steel plate supplier mill at Gangsteel Group.

SA516GR65,ASTM SA516GR65,SA516GR65 Steel Plate,SA516GR65 HIC, SA516GR65 NACE

Tags: SA516GR65,ASTM SA516GR65,SA516GR65 Steel Plate,SA516GR65 steel factory, SA516GR65 adopt standard, SA516GR65 Heat treatment, SA516GR65 Technical delivery condition, SA516GR65 Chemical, SA516GR65 Mechanical property, SA516GR65 Price, SA516GR65 CEV, SA516GR65 Impact degree, SA516GR65 impact energy, SA516GR65 Supplier,SA516GR65 Specification, SA516GR65 properties, Material SA516GR65 N, SA516GR65 Material, ASME SA516GR65, SA516GR65 Steel, SA516GR65 Yield, SA516GR65 plate, SA516GR65 HIC, SA516GR65 NACE MR0175, SA516GR65 ISO 15156, SA516GR65 NACE MR0103, SA516GR65 SSC

Keyword: SA516GR65,ASME SA516GR65,SA516GR65 Steel,SA516GR65 HIC, SA516GR65 NACE

- SA516GR65 Adopt standard: ASME SA516 Standard Specification for High-Strength Low-Alloy Columbium-Vanadium Structural Steel

- SA516GR65 Specification:  Thickness: 1mm to 100mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

- Third Party Inspection for SA516GR65: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

- SA516GR65 Chemical composition % of the Product analysis of grade

| Grade | SA516Gr.65 Chemical Composition, Max (%) |
| --- | --- |
|  | C | Si | Mn | P | S |
| SA516Gr65 | 0.24-0.29 | 0.13-0.45 | 0.79-1.30 | 0.035 | 0.035 |

- SA516GR65 Mechanical Property

| Grade | SA516Gr65 Mechanical Property |
| --- | --- |
|  | Thickness | Yield | Tensile | Elongation |
| SA516Gr65 | mm | Min Mpa | Mpa | Min % |
|  | 5-40 | 240 | 450-585 | 23% |
|  | 40-100 | 240 | 450-585 | 19% |

- SA516GR65 Delivery Time Or Lead Time: 15-30days

- SA516GR65 Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

- If you have any requirement in steel plate for SA516GR65, whether the new plate or stock list of material, please feel free to contact us by email of calling.

- If you had any question at our plate or service. Please contact our after service department to get faster reply.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting ASME SA516 SA516GR65 NACE MR0175, MR0103 Boiler steel plate, Low alloy and high strength steel plate,                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                  heavy plate and wide, heavy plate, Which is a large steel plate supplier mill at Gangsteel Group.

SA516GR65,ASTM SA516GR65,SA516GR65 Steel Plate,SA516GR65 HIC, SA516GR65 NACE

Tags: SA516GR65,ASTM SA516GR65,SA516GR65 Steel Plate,SA516GR65 steel factory, SA516GR65 adopt standard, SA516GR65 Heat treatment, SA516GR65 Technical delivery condition, SA516GR65 Chemical, SA516GR65 Mechanical property, SA516GR65 Price, SA516GR65 CEV, SA516GR65 Impact degree, SA516GR65 impact energy, SA516GR65 Supplier,SA516GR65 Specification, SA516GR65 properties, Material SA516GR65 N, SA516GR65 Material, ASME SA516GR65, SA516GR65 Steel, SA516GR65 Yield, SA516GR65 plate, SA516GR65 HIC, SA516GR65 NACE MR0175, SA516GR65 ISO 15156, SA516GR65 NACE MR0103, SA516GR65 SSC