SA537 CLASS 2 MR0175,SA537 CLASS 2 Steel,SA537 CLASS 2 HIC,SA537 CLASS 2 NACE

Gangsteel Bolier Plate Factory are specialized in producing and exporting ASME SA537 SA537 CLASS 2 NACE MR0175, MR0103 Boiler steel plate, Low alloy and high strength steel plate,                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                  heavy plate and wide, heavy plate, Which is a large steel plate supplier mill at Gangsteel Group.

SA537 CLASS 2,ASTM SA537 CLASS 2,SA537 CLASS 2 Steel Plate,SA537 CLASS 2 HIC,SA537 CLASS 2 Nace

Tags: SA537 CLASS 2,ASTM SA537 CLASS 2,SA537 CLASS 2 Steel Plate,SA537 CLASS 2 steel factory, SA537 CLASS 2 adopt standard, SA537 CLASS 2 Heat treatment, SA537 CLASS 2 Technical delivery condition, SA537 CLASS 2 Chemical, SA537 CLASS 2 Mechanical property, SA537 CLASS 2 Price, SA537 CLASS 2 CEV, SA537 CLASS 2 Impact degree, SA537 CLASS 2 impact energy, SA537 CLASS 2 Supplier,SA537 CLASS 2 Specification, SA537 CLASS 2 properties, Material SA537 CLASS 2 N, SA537 CLASS 2 Material, ASME SA537 CLASS 2, SA537 CLASS 2 Steel, SA537 CLASS 2 Yield, SA537 CLASS 2 plate, SA537 CLASS 2 HIC, SA537 CLASS 2 NACE MR0175, SA537 CLASS 2 ISO 15156, SA537 CLASS 2 NACE MR0103, SA537 CLASS 2 SSC

Keyword: SA537 CLASS 2,ASME SA537 CLASS 2,SA537 CLASS 2 Steel,SA537 CLASS 2 HIC,SA537 CLASS 2 NACE

- SA537 CLASS 2 Adopt standard: ASME SA537 Standard Specification for High-Strength Low-Alloy Columbium-Vanadium Structural Steel

- SA537 CLASS 2 Specification:  Thickness: 1mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

- Third Party Inspection for SA537 CLASS 2: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

- SA537 CLASS 2 Chemical composition % of the Product analysis of grade

| Grade | C % | Si % | Mn % | P % | S % | V % | AL % | Cr % |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SA537 CLASS 2 | 0.24 | 0.13-0.55 | 0.64-1.46 | 0.035 | 0.035 |  |  | 0.29 |
|  | Cu % | Mo % | Nb % | Ni % | Ti % |  |  |  |
|  | 0.38 | 0.09 |  | 0.28 |  |  |  |  |

- SA537 CLASS 2 Mechanical Property

| Grade | THK.(mm) | Min Yield | Tensile | Elongation | Min Impact Energy |
| --- | --- | --- | --- | --- | --- |
| SA537 CLASS 2 | 5-65 | 415 Mpa | 550-690 Mpa | 22% |  |  |
|  | 65-100 | 380 Mpa | 515-655 Mpa | 20% |  |  |
|  | 100-150 | 315 Mpa | 485-620 Mpa |  |  |  |

Normally ASME SA537 CLASS 2 plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

ASME SA537 CLASS 2 steel plates shall be normalized. SA537 CLASS 2 and SA537Cl3 plates shall be quenched and tempered. The tempering temperature for Cl2 plates shall not be less than 1100°F [595°C] for not less than 1⁄2 h and 1150°F [620°C] for Class 3 plates for not less than 1⁄2 h.

- SA537 CLASS 2 Delivery Time Or Lead Time: 15-30days

- SA537 CLASS 2 Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

- If you have any requirement in steel plate for SA537 CLASS 2, whether the new plate or stock list of material, please feel free to contact us by email of calling.

- If you had any question at our plate or service. Please contact our after service department to get faster reply.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting ASME SA537 SA537 CLASS 2 NACE MR0175, MR0103 Boiler steel plate, Low alloy and high strength steel plate,                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                  heavy plate and wide, heavy plate, Which is a large steel plate supplier mill at Gangsteel Group.

SA537 CLASS 2,ASTM SA537 CLASS 2,SA537 CLASS 2 Steel Plate,SA537 CLASS 2 HIC,SA537 CLASS 2 Nace

Tags: SA537 CLASS 2,ASTM SA537 CLASS 2,SA537 CLASS 2 Steel Plate,SA537 CLASS 2 steel factory, SA537 CLASS 2 adopt standard, SA537 CLASS 2 Heat treatment, SA537 CLASS 2 Technical delivery condition, SA537 CLASS 2 Chemical, SA537 CLASS 2 Mechanical property, SA537 CLASS 2 Price, SA537 CLASS 2 CEV, SA537 CLASS 2 Impact degree, SA537 CLASS 2 impact energy, SA537 CLASS 2 Supplier,SA537 CLASS 2 Specification, SA537 CLASS 2 properties, Material SA537 CLASS 2 N, SA537 CLASS 2 Material, ASME SA537 CLASS 2, SA537 CLASS 2 Steel, SA537 CLASS 2 Yield, SA537 CLASS 2 plate, SA537 CLASS 2 HIC, SA537 CLASS 2 NACE MR0175, SA537 CLASS 2 ISO 15156, SA537 CLASS 2 NACE MR0103, SA537 CLASS 2 SSC