A283GRA,A283GRA Steel Plate,A283GRA Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting A283/A283M A283GRA NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. A283GRA,A283/A283M A283GRA,A283GRA Steel Plate,A283GRA HIC,A283GRA Nace

Tags: A283GRA,A283/A283M A283GRA,A283GRA Steel Plate,A283GRA steel factory, A283GRA adopt standard, A283GRA Heat treatment, A283GRA Technical delivery condition, A283GRA Chemical, A283GRA Mechanical property, A283GRA Price, A283GRA CEV, A283GRA Impact degree, A283GRA impact energy, A283GRA Supplier,A283GRA Specification, A283GRA properties, Material A283GRA N, A283GRA Material, A283/A283M, A283GRA Steel, A283GRA Yield, A283GRA plate, A283GRA HIC, A283GRA NACE MR0175, A283GRA ISO 15156, A283GRA NACE MR0103, A283GRA SSC

Keyword: A283GRA,A283GRA Steel Plate,A283GRA Supplier

1.  A283GRA Adopt standard: ASMT A283/A283M Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon

2.  A283GRA Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for A283GRA: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  A283GRA Chemical composition % of the Product analysis of grade

| Grade | C % | Mn % | P% | S% | Cu%(min) | Cu%(<=40mm) | Cu%(>40mm) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| A283GRA | 0.14 | 0.9 | 0.035 | 0.04 | 0.2 | 0.4 | 0.15-0.4 |

5.  A283GRA Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| A283GRA | 165 Mpa | 301-450Mpa | <=50MM | 30% |
|  | 165Mpa | 310-415Mpa | 50-200MM | 27% |

6.  Normally A283/A283M A283GRA plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  A283GRA Delivery Time Or Lead Time: 20-35days

8.  A283GRA Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for A283GRA, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting A283/A283M A283GRA NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. A283GRA,A283/A283M A283GRA,A283GRA Steel Plate,A283GRA HIC,A283GRA Nace

Tags: A283GRA,A283/A283M A283GRA,A283GRA Steel Plate,A283GRA steel factory, A283GRA adopt standard, A283GRA Heat treatment, A283GRA Technical delivery condition, A283GRA Chemical, A283GRA Mechanical property, A283GRA Price, A283GRA CEV, A283GRA Impact degree, A283GRA impact energy, A283GRA Supplier,A283GRA Specification, A283GRA properties, Material A283GRA N, A283GRA Material, A283/A283M, A283GRA Steel, A283GRA Yield, A283GRA plate, A283GRA HIC, A283GRA NACE MR0175, A283GRA ISO 15156, A283GRA NACE MR0103, A283GRA SSC