GB/T 713 12Cr2MoLR, 12Cr2MoLR STEEL PLATE,12Cr2MoLR Boiler steel plate

Gangsteel Bolier Plate Factory are specialized in producing and exporting GB/T 713 12Cr2MoLR NACE MR0175, MR0103 Boiler steel plate, Low alloy and high strength steel plate,                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                  heavy plate and wide, heavy plate, Which is a large steel plate supplier mill at Gangsteel Group.

12Cr2MoLR,GB/T 713 12Cr2MoLR,12Cr2MoLR Steel Plate,12Cr2MoLR HIC,12Cr2MoLR Nace

Tags: 12Cr2MoLR,GB/T 713 12Cr2MoLR,12Cr2MoLR Steel Plate,12Cr2MoLR steel factory, 12Cr2MoLR adopt standard, 12Cr2MoLR Heat treatment, 12Cr2MoLR Technical delivery condition, 12Cr2MoLR Chemical, 12Cr2MoLR Mechanical property, 12Cr2MoLR Price, 12Cr2MoLR CEV, 12Cr2MoLR Impact degree, 12Cr2MoLR impact energy, 12Cr2MoLR Supplier,12Cr2MoLR Specification, 12Cr2MoLR properties, Material 12Cr2MoLR N, 12Cr2MoLR Material, GB/T 713, 12Cr2MoLR Steel, 12Cr2MoLR Yield, 12Cr2MoLR plate, 12Cr2MoLR HIC, 12Cr2MoLR NACE MR0175, 12Cr2MoLR ISO 15156, 12Cr2MoLR NACE MR0103, 12Cr2MoLR SSC

Keyword: 12Cr2MoLR,GB/T 713 12Cr2MoLR,12Cr2MoLR Steel,12Cr2MoLR HIC,12Cr2MoLR NACE

- 12Cr2MoLR Adopt standard: GB/T 713 Standard Specification for boiler and pressure purposes, technical delivery condition and non alloy, alloy steels with specified elevated temperature properties.

- 12Cr2MoLR Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

- Third Party Inspection for 12Cr2MoLR: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

- 12Cr2MoLR Chemical composition % of the Product analysis of grade

| Grade | C % | Si % | Mn % | Cu % | Ni % | Cr% | Mo % | V % |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 12Cr2MoLR | 0.08-0.15 | 0.5 | 0.3-0.6 | 0.2 | 0.3 | 2.0-2.5 | 0.9-1.0 | -- |
|  | Ti % | Alt % | P % | S % | Nb |  |  |  |
|  | -- | -- | 0.02 | 0.01 | -- |  |  |  |

- 12Cr2MoLR Mechanical Property

| Grade | Thickness(mm) | Min Yield | Tensile | Elongation | Min Impact Energy |
| --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | Degree | Min J |
| 12Cr2MoLR | 6-200 | 310 Mpa | 520-680 Mpa | 19% | 20 | 47J |

Normally GB/T 713 12Cr2MoLR plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

- 12Cr2MoLR Delivery Time Or Lead Time: 20-35days

- 12Cr2MoLR Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

- If you have any requirement in steel plate for 12Cr2MoLR, whether the new plate or stock list of material, please feel free to contact us by email of calling.

- If you had any question at our plate or service. Please contact our after service department to get faster reply.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting GB/T 713 12Cr2MoLR NACE MR0175, MR0103 Boiler steel plate, Low alloy and high strength steel plate,                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                  heavy plate and wide, heavy plate, Which is a large steel plate supplier mill at Gangsteel Group.

12Cr2MoLR,GB/T 713 12Cr2MoLR,12Cr2MoLR Steel Plate,12Cr2MoLR HIC,12Cr2MoLR Nace

Tags: 12Cr2MoLR,GB/T 713 12Cr2MoLR,12Cr2MoLR Steel Plate,12Cr2MoLR steel factory, 12Cr2MoLR adopt standard, 12Cr2MoLR Heat treatment, 12Cr2MoLR Technical delivery condition, 12Cr2MoLR Chemical, 12Cr2MoLR Mechanical property, 12Cr2MoLR Price, 12Cr2MoLR CEV, 12Cr2MoLR Impact degree, 12Cr2MoLR impact energy, 12Cr2MoLR Supplier,12Cr2MoLR Specification, 12Cr2MoLR properties, Material 12Cr2MoLR N, 12Cr2MoLR Material, GB/T 713, 12Cr2MoLR Steel, 12Cr2MoLR Yield, 12Cr2MoLR plate, 12Cr2MoLR HIC, 12Cr2MoLR NACE MR0175, 12Cr2MoLR ISO 15156, 12Cr2MoLR NACE MR0103, 12Cr2MoLR SSC