A387GR9,A387GR9 Steel Plate,A387GR9 Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting A387/A387M A387GR9 NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Molybdenum Which is a large steel plate supplier mill at Gangsteel Group. A387GR9,A387/A387M A387GR9,A387GR9 Steel Plate,A387GR9 HIC,A387GR9 Nace

Tags: A387GR9,A387/A387M A387GR9,A387GR9 Steel Plate,A387GR9 steel factory, A387GR9 adopt standard, A387GR9 Heat treatment, A387GR9 Technical delivery condition, A387GR9 Chemical, A387GR9 Mechanical property, A387GR9 Price, A387GR9 CEV, A387GR9 Impact degree, A387GR9 impact energy, A387GR9 Supplier,A387GR9 Specification, A387GR9 properties, Material A387GR9 N, A387GR9 Material, A387/A387M, A387GR9 Steel, A387GR9 Yield, A387GR9 plate, A387GR9 HIC, A387GR9 NACE MR0175, A387GR9 ISO 15156, A387GR9 NACE MR0103, A387GR9 SSC

Keyword: A387GR9,A387GR9 Steel Plate,A387GR9 Supplier

1.  A387GR9 Adopt standard: ASMT A387/A387M Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Molybdenum

2.  A387GR9 Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for A387GR9: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  A387GR9 Chemical composition % of the Product analysis of grade

| Grade | C % | Mn % | P% | S% | Si% | Cr% | Mo% | Ni% |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| A387GR9 | 0.15 | 0.25-0.66 | 0.030 | 0.03 | 1.05 | 7.9-10.1 | 0.85-1.15 | -- |
|  | V% | Cb% | B% | N% | Al% | W% |  |  |
|  | -- | -- | -- | -- | -- | -- |  |  |

5.  A387GR9 Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| A387GR9 | 205Mpa | 415-585Mpa | <=50MM | 18% |
|  | 205Mpa | 415-585Mpa | 50-200MM | -- |

6.  Normally A387/A387M A387GR9 plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  A387GR9 Delivery Time Or Lead Time: 20-35days

8.  A387GR9 Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for A387GR9, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting A387/A387M A387GR9 NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. A387GR9,A387/A387M A387GR9,A387GR9 Steel Plate,A387GR9 HIC,A387GR9 Nace

Tags: A387GR9,A387/A387M A387GR9,A387GR9 Steel Plate,A387GR9 steel factory, A387GR9 adopt standard, A387GR9 Heat treatment, A387GR9 Technical delivery condition, A387GR9 Chemical, A387GR9 Mechanical property, A387GR9 Price, A387GR9 CEV, A387GR9 Impact degree, A387GR9 impact energy, A387GR9 Supplier,A387GR9 Specification, A387GR9 properties, Material A387GR9 N, A387GR9 Material, A387/A387M, A387GR9 Steel, A387GR9 Yield, A387GR9 plate, A387GR9 HIC, A387GR9 NACE MR0175, A387GR9 ISO 15156, A387GR9 NACE MR0103, A387GR9 SSC