A710GRA,A710GRA Steel Plate,A710GRA Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting A710/A710M A710GRA NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Precipitation-Strengthened Low-Carbon Nickel-copper-Chromium-Molybdenum-Columbium Alloy Structural Steel Plates, Which is a large steel plate supplier mill at Gangsteel Group. A710GRA,A710/A710M A710GRA,A710GRA Steel Plate,A710GRA HIC,A710GRA Nace

Tags: A710GRA,A710/A710M A710GRA,A710GRA Steel Plate,A710GRA steel factory, A710GRA adopt standard, A710GRA Heat treatment, A710GRA Technical delivery condition, A710GRA Chemical, A710GRA Mechanical property, A710GRA Price, A710GRA CEV, A710GRA Impact degree, A710GRA impact energy, A710GRA Supplier,A710GRA Specification, A710GRA properties, Material A710GRA N, A710GRA Material, A710/A710M, A710GRA Steel, A710GRA Yield, A710GRA plate, A710GRA HIC, A710GRA NACE MR0175, A710GRA ISO 15156, A710GRA NACE MR0103, A710GRA SSC

Keyword: A710GRA,A710GRA Steel Plate,A710GRA Supplier

1.  A710GRA Adopt standard: ASMT A710/A710M Standard Specification for Precipitation-Strengthened Low-Carbon Nickel-copper-Chromium-Molybdenum-Columbium Alloy Structural Steel Plates.

2.  A710GRA Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for A710GRA: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  A710GRA Chemical composition % of the Product analysis of grade

| Grade | C % | Mn % | P% | S% | Si% | Ni% |
| --- | --- | --- | --- | --- | --- | --- |
| A710GRA | 0.07 | 0.40-0.70 | 0.025 | 0.025 | 0.4 | 0.7-1.0 |
|  | Mo% | Cu% | Cb% | Ti% | Cr% |  |
|  | 0.15-0.25 | 1.0-1.3 | 0.02 | -- | 0.6-0.9 |  |

5.  A710GRA Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| A710GRA | 550Mpa | 585Mpa | <6.5mm | 20% |
|  | 585Mpa | 585Mpa | 6.5-8mm | 20% |
|  | 550Mpa | 585Mpa | 8-10mm | 20% |
|  | 550Mpa | 585Mpa | 10-12.5mm | 20% |
|  | 550Mpa | 585Mpa | 12.5-20mm | 20% |
|  | 550Mpa | 585Mpa | 20-25mm | 20% |
|  | 550Mpa | 585Mpa | 25-30mm | 20% |
|  | 515Mpa | 585Mpa | 30-50mm | 20% |
|  | 450Mpa | 515Mpa | 50-100mm | -- |
|  | 415Mpa | 485Mpa | >100mm | -- |

6.  Normally A710/A710M A710GRA plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  A710GRA Delivery Time Or Lead Time: 20-35days

8.  A710GRA Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for A710GRA, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting A710/A710MA710GRA NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. A710GRA,A710/A710M A710GRA,A710GRA Steel Plate,A710GRA HIC,A710GRA Nace

Tags: A710GRA,A710/A710M A710GRA,A710GRA Steel Plate,A710GRA steel factory, A710GRA adopt standard, A710GRA Heat treatment, A710GRA Technical delivery condition, A710GRA Chemical, A710GRA Mechanical property, A710GRA Price, A710GRA CEV, A710GRA Impact degree, A710GRA impact energy, A710GRA Supplier,A710GRA Specification, A710GRA properties, Material A710GRA N, A710GRA Material, A710/A710M, A710GRA Steel, A710GRA Yield, A710GRA plate, A710GRA HIC, A710GRA NACE MR0175, A710GRA ISO 15156, A710GRA NACE MR0103, A710GRA SSC