A841GRA,A841GRA Steel Plate,A841GRA Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA-841/SA-841M A841GRA NACE MR0175, MR0103 Boiler steel plate, Specification for Steel plates for pressure vessels,produced by the thermo mechanical control process(TMCP) Which is a large steel plate supplier mill at Gangsteel Group. A841GRA,SA-841/SA-841M A841GRA,A841GRA Steel Plate,A841GRA HIC,A841GRA Nace

Tags: A841GRA,SA-841/SA-841M A841GRA,A841GRA Steel Plate,A841GRA steel factory, A841GRA adopt standard, A841GRA Heat treatment, A841GRA Technical delivery condition, A841GRA Chemical, A841GRA Mechanical property, A841GRA Price, A841GRA CEV, A841GRA Impact degree, A841GRA impact energy, A841GRA Supplier,A841GRA Specification, A841GRA properties, Material A841GRA N, A841GRA Material, SA-841/SA-841M, A841GRA Steel, A841GRA Yield, A841GRA plate, A841GRA HIC, A841GRA NACE MR0175, A841GRA ISO 15156, A841GRA NACE MR0103, A841GRA SSC

Keyword: A841GRA,A841GRA Steel Plate,A841GRA Supplier

1.  A841GRA Adopt standard: ASMT SA-841/SA-841M Specification for Steel plates for pressure vessels,produced by the thermo mechanical control process(TMCP)

2.  A841GRA Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for A841GRA: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  A841GRA Chemical composition % of the Product analysis of grade

| Grade | C % | Mn %(<40mm) | P% | S% | Si% | Cu% | Ni% | Cr% |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| A841GRA | 0.2 | 0.7-1.35 | 0.03 | 0.03 | 0.15-0.5 | 0.35 | 0.25 | 0.25 |
|  | Mo% | Cb% | V% | Mn %(>40mm) | Ti% | B% |  |  |
|  | 0.08 | 0.03 | 0.06 | 1.0-1.6 | -- | -- |  |  |

5.  A841GRA Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| A841GRA | 345 Mpa | 480-620Mpa | <40MM | 22% |
|  | 345 Mpa | 480-620Mpa | 40-65MM | 22% |
|  | 310 Mpa | 450-585Mpa | >65MM | 22% |

6.  Normally SA-841/SA-841M A841GRA plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  A841GRA Delivery Time Or Lead Time: 20-35days

8.  A841GRA Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for A841GRA, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA-841/SA-841M A841GRA NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. A841GRA,SA-841/SA-841M A841GRA,A841GRA Steel Plate,A841GRA HIC,A841GRA Nace

Tags: A841GRA,SA-841/SA-841M A841GRA,A841GRA Steel Plate,A841GRA steel factory, A841GRA adopt standard, A841GRA Heat treatment, A841GRA Technical delivery condition, A841GRA Chemical, A841GRA Mechanical property, A841GRA Price, A841GRA CEV, A841GRA Impact degree, A841GRA impact energy, A841GRA Supplier,A841GRA Specification, A841GRA properties, Material A841GRA N, A841GRA Material, SA-841/SA-841M, A841GRA Steel, A841GRA Yield, A841GRA plate, A841GRA HIC, A841GRA NACE MR0175, A841GRA ISO 15156, A841GRA NACE MR0103, A841GRA SSC