SA710 GRADE A,SA710 GRADE A Steel Plate,SA710 GRADE A Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA710/SA710M SA710 GRADE A NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Precipitation-Strengthened Low-Carbon Nickel-copper-Chromium-Molybdenum-Columbium Alloy Structural Steel Plates, Which is a large steel plate supplier mill at Gangsteel Group. SA710 GRADE A,SA710/SA710M SA710 GRADE A,SA710 GRADE A Steel Plate,SA710 GRADE A HIC,SA710 GRADE A Nace

Tags: SA710 GRADE A,SA710/SA710M SA710 GRADE A,SA710 GRADE A Steel Plate,SA710 GRADE A steel factory, SA710 GRADE A adopt standard, SA710 GRADE A Heat treatment, SA710 GRADE A Technical delivery condition, SA710 GRADE A Chemical, SA710 GRADE A Mechanical property, SA710 GRADE A Price, SA710 GRADE A CEV, SA710 GRADE A Impact degree, SA710 GRADE A impact energy, SA710 GRADE A Supplier,SA710 GRADE A Specification, SA710 GRADE A properties, Material SA710 GRADE A N, SA710 GRADE A Material, SA710/SA710M, SA710 GRADE A Steel, SA710 GRADE A Yield, SA710 GRADE A plate, SA710 GRADE A HIC, SA710 GRADE A NACE MR0175, SA710 GRADE A ISO 15156, SA710 GRADE A NACE MR0103, SA710 GRADE A SSC

Keyword: SA710 GRADE A,SA710 GRADE A Steel Plate,SA710 GRADE A Supplier

1.  SA710 GRADE A Adopt standard: ASME SA710/SA710M Standard Specification for Precipitation-Strengthened Low-Carbon Nickel-copper-Chromium-Molybdenum-Columbium Alloy Structural Steel Plates.

2.  SA710 GRADE A Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for SA710 GRADE A: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  SA710 GRADE A Chemical composition % of the Product analysis of grade

| Grade | C % | Mn % | P% | S% | Si% | Ni% |
| --- | --- | --- | --- | --- | --- | --- |
| SA710 GRADE A | 0.07 | 0.40-0.70 | 0.025 | 0.025 | 0.4 | 0.7-1.0 |
|  | Mo% | Cu% | Cb% | Ti% | Cr% |  |
|  | 0.15-0.25 | 1.0-1.3 | 0.02 | -- | 0.6-0.9 |  |

5.  SA710 GRADE A Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| SA710 GRADE A | 550Mpa | 585Mpa | <6.5mm | 20% |
|  | 585Mpa | 585Mpa | 6.5-8mm | 20% |
|  | 550Mpa | 585Mpa | 8-10mm | 20% |
|  | 550Mpa | 585Mpa | 10-12.5mm | 20% |
|  | 550Mpa | 585Mpa | 12.5-20mm | 20% |
|  | 550Mpa | 585Mpa | 20-25mm | 20% |
|  | 550Mpa | 585Mpa | 25-30mm | 20% |
|  | 515Mpa | 585Mpa | 30-50mm | 20% |
|  | 450Mpa | 515Mpa | 50-100mm | -- |
|  | 415Mpa | 485Mpa | >100mm | -- |

6.  Normally SA710/SA710M SA710 GRADE A plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  SA710 GRADE A Delivery Time Or Lead Time: 20-35days

8.  SA710 GRADE A Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for SA710 GRADE A, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA710/SA710MSA710 GRADE A NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. SA710 GRADE A,SA710/SA710M SA710 GRADE A,SA710 GRADE A Steel Plate,SA710 GRADE A HIC,SA710 GRADE A Nace

Tags: SA710 GRADE A,SA710/SA710M SA710 GRADE A,SA710 GRADE A Steel Plate,SA710 GRADE A steel factory, SA710 GRADE A adopt standard, SA710 GRADE A Heat treatment, SA710 GRADE A Technical delivery condition, SA710 GRADE A Chemical, SA710 GRADE A Mechanical property, SA710 GRADE A Price, SA710 GRADE A CEV, SA710 GRADE A Impact degree, SA710 GRADE A impact energy, SA710 GRADE A Supplier,SA710 GRADE A Specification, SA710 GRADE A properties, Material SA710 GRADE A N, SA710 GRADE A Material, SA710/SA710M, SA710 GRADE A Steel, SA710 GRADE A Yield, SA710 GRADE A plate, SA710 GRADE A HIC, SA710 GRADE A NACE MR0175, SA710 GRADE A ISO 15156, SA710 GRADE A NACE MR0103, SA710 GRADE A SSC