S235JR S355JR S355J2 IPE Beams (I Sections)

1.Structural Steel Sections

Universal Columns (UC) | Universal Beams (UB) | Parallel Flange Steel Channels (PFC)

Hot Rolled Steel Angles (RSA) | IPE Beams (I sections) | UPN Channels (U sections)

H Section Steel

2.We specialise in the supply of IPE steel sections including IPE Beams (I Sections). Unlike Universal Beams (UB), which use UK measurements, IPE Beams (also known as 'I Sections') are truly metric.

3.We supply a wide range of Continental Beams from IPE80 to IPE600. Our high yield IPE Beams are excellent for working in cold temperatures. Low temperature testing is available and can be carried out at your designated temperature ie. -20°C, -30°C, -50°C.

4.Standards/Grades

EN 10025 S235

EN 10025 S355

Please refer to the specification table below. To receive more information regarding IPE Beams (I Sections) or request a competitive quotation, please contact us

| Mass per metre KG/M | Metric Dimensions | Thicknesses |
| --- | --- | --- |
|  | Section Depth (mm) | Section Width (mm) | Web (mm) | Flange (mm) |
| IPE 80 | 6 | 80 | 46 | 38 | 5.2 |
| IPE 100 | 8.1 | 100 | 55 | 4.1 | 5.7 |
| IPE 120 | 10.4 | 120 | 64 | 4.4 | 6.3 |
| IPE 140 | 12.9 | 140 | 73 | 4.7 | 6.9 |
| IPE 160 | 15.8 | 160 | 82 | 5 | 7.4 |
| IPE 180 | 18.8 | 180 | 91 | 5.3 | 8 |
| IPE 200 | 22.4 | 200 | 100 | 5.6 | 8.5 |
| IPE 220 | 26.2 | 220 | 110 | 5.9 | 9.2 |
| IPE 240 | 30.7 | 240 | 120 | 6.2 | 9.8 |
| IPE 270 | 36.1 | 270 | 135 | 6.6 | 10.2 |
| IPE 300 | 42.2 | 300 | 150 | 7.1 | 10.7 |
| IPE 330 | 49.1 | 330 | 160 | 7.5 | 11.5 |
| IPE 360 | 57.1 | 360 | 170 | 8 | 12.7 |
| IPE 400 | 66.3 | 400 | 180 | 8.6 | 13.5 |
| IPE 450 | 7.6 | 450 | 190 | 9.4 | 14.6 |
| IPE 500 | 90.7 | 500 | 200 | 10.2 | 16 |
| IPE 550 | 106 | 550 | 210 | 11.1 | 17.2 |
| IPE 600 | 122 | 600 | 220 | 12 | 19 |