S235JR S355JR S355J2 Parallel Flange Rolled Steel Channels (PFC)

1.Structural Steel Sections

Universal Columns (UC) | Universal Beams (UB) | Parallel Flange Steel Channels (PFC)

Hot Rolled Steel Angles (RSA) | IPE Beams (I sections) | UPN Channels (U sections)

H Section Steel

2.Whilst we supply an extensive range, we particularly excel in supplying channels which are ideal for use in high yield – low working temperatures. Low temperature impact testing is available across the range.

3.Standards/Grades

EN 10025 S275

EN 10025 S355

For further information, please refer to the sizes/specification table below. To find our more about Parallel Flange Rolled Steel Channels (PFC) receive a detailed and competitive quotation, please contact us.

| Designation Serial Size MM | Mass per Metre kg/m | Metric Dimensions | Thicknesses |
| --- | --- | --- | --- |
|  |  | Section Depth | Section Width | Web (mm) | Flange (mm) |
| 100 x 50 x 10 | 10.2 | 100 | 50 | 5 | 8.5 |
| 125 x 65 x 15 | 14.8 | 125 | 65 | 5.5 | 9.5 |
| 150 x 75 x 18 | 17.9 | 150 | 75 | 5.5 | 10 |
| 150 x 90 x 24 | 23.9 | 150 | 90 | 6.5 | 12 |
| 180 x 75 x 20 | 20.3 | 180 | 75 | 6 | 10.5 |
| 180 x 90 x 26 | 26.1 | 180 | 90 | 6.5 | 12.5 |
| 200 x 75 x 23 | 23.4 | 200 | 75 | 6 | 12.5 |
| 200 x 90 x 30 | 29.7 | 200 | 90 | 7 | 14 |
| 230 x 75 x 26 | 25.7 | 230 | 75 | 6.5 | 12.5 |
| 230 x 90 x 32 | 32.2 | 230 | 90 | 7.5 | 14 |
| 260 x 75 x 28 | 27.6 | 260 | 75 | 7 | 12 |
| 260 x 90 x 35 | 34.8 | 260 | 90 | 8 |  |
| 300 x 90 x 41 | 41.4 | 300 | 90 | 9 |  |
| 300 x 100 x 46 | 45.5 | 300 | 10 | 9 |  |
| 380 x 100 x 54 | 54 | 380 | 100 | 9.5 |  |
| 430 x 100 x 64 | 64.4 | 430 | 100 | 11 |  |